FY2016 Contract Seal Coat Guidelines

- Plans, Specifications and Estimate

  - Plan templates are located in ProjectWise in the design seed files:

SEAL_COAT_01_Title_06_2015

SEAL_COAT_02_Typical_06_2015

SEAL_COAT_03_Quantities_06_2015

SEAL_COAT_04_TC_06_2015

SEAL_COAT_05_TC_06_2015

SEAL_COAT_06_TC_06_2015

The ADT of the routes should be listed in the left top corner of the Title sheet.  This information is used by the Project Reviewer to set the liquidated damages and is also beneficial to the contractor to be aware of the amount of traffic on the route.

- Selection guidance on the aggregate grade of seal coat will be as follows:

The type of bituminous material and grade of liquid asphalt is selected by the contractor. Differing aggregate qualities are available and specified according to the roadway traffic as shown in the tables below:

| Two Way Traffic |  |
| --- | --- |
| Seal Coat Grade | ADT |
| C | < 750 and any shoulders |
| B1 & B2 | < 1,700 |
| A1 | < 3,500 |
| A2 | < 8,500 |

| Divided Highways |  |
| --- | --- |
| Seal Coat Grade | ADT |
| B1 & B2 | < 3,500 |
| A1 | < 14,000 |
| A2 | < 17,000 |

Grades A1 and B1 are coarse (3/8”) aggregate seals and should be used on pavement surfaces with minor distresses.

Grades A2 and B2 are fine (1/4”) aggregate seals and should be used on pavement surfaces with little to no distresses.

To improve the perception of the driving public, Sec 409 requires the finished seal coat to have a dark appearance.  See EPG 751.1.3.6 Asphalt Wearing Surface for guidelines on aggregate grade selection for bridges.

A seal coat placed on a porous surface such as an aggregate base should receive a prime coat.

- The JSP template is located in EPG 409 Seal Coat Program.

- Any surface irregularities will be accounted for by adjusting the application rate in the field per the direction of the Engineer.  No additional quantities should be accounted for in the plans.

- Pavement Marking:  The pavement marking is to be performed by MoDOT forces. The District will need to coordinate with the striping crews to have the stripe completed within 14 days after the seal coat is completed.

Routes that have an existing edgeline, will need to include quantities for Type 1 Temporary Raised Pavement Markers for the edgeline in addition to the centerline marking.

- The contract time will need to be specified in the Contract Liquidated Damages JSP.  The general rule is two (2) calendar days for every one (1) working day with a minimum of 30 calendar days unless the district has justification for a tighter time frame due to impacts to the traveling public.  Calendar days for each route should be included in the PS&E submittal.

Recommended Completion Date:  	September 1, 2016

Recommended Completion Date if let after March 31, 2016:	September 1, 2017

For projects with a 2017 completion date, Seal Coat Completion of Work JSP (JSP-15-08) must be included in the JSPs. Additionally; the RE will be responsible to advise maintenance staff of the contractor proposed completion date in order to address any impacts to maintenance activities performed in effort to prepare the route for the contract treatment.

- Bridges:  Bridges should be excepted unless prior written approval is obtained from the Bridge Division and submitted with the transmittal package.

| MoDOT STRIPING |  |
| --- | --- |
| Item No. | Description |
| 4091048 | Emulsified Asphalt, Seal Coat |
| 40940XX | Seal Coat Aggregate, Grade A1, A2, B1, B2, or C |
| 6161005 | Construction Signs |
| 6161009 | Flag Assemblies |
| 6208064 | Temporary Raised Pavement Marker, Type 1 |

Note:  Do not include Mobilization