EPOXY WET REFLECTIVE PAVEMENT MARKINGS

1.0  Description.  This work shall consist of furnishing and installing wet reflective pavement markings as shown on the plans or as directed by the engineer.  The pavement markings shall consist of an epoxy pavement marking paint, MoDOT Type P glass beads, and wet reflective pavement marking beads.  The beads shall be placed as a double drop system to provide wet night retroreflectivity.  This work shall be in accordance with Sec 620 and accompanying provisions except as modified herein.

2.0  Material.  All material shall be in accordance with Division 1000, Material Details, and specifically as follows.

| ## Item | ## Section |
| --- | --- |
| Type P Drop-On Glass Beads | 1048.40 |
| Epoxy Pavement Marking Material | 1048.60 |

2.1 Wet Reflective Beads.  The wet reflective beads used shall be from the following approved products list:

| Manufacturer | Product |
| --- | --- |
| 3M Inc. | All Weather Elements |
| Potters Industries, Inc. | Visimax |
| Swarco | Plus-9-Spots |

3.0   Construction Requirements.

3.1  Application of the wet reflective marking shall consist of placement of the epoxy paint, followed by the application of Type P glass beads and the wet reflective beads.  The color of the wet reflective beads shall match the color of the line being applied.

3.2  The width of the line shall be as shown on the plans.

3.3  The epoxy paint shall be applied at a minimum thickness of 20 mils.  The thickness may be increased depending on manufacturer’s recommendations to properly hold the bead system.

3.4  Type P glass beads and the wet reflective beads shall be mechanically applied to the wet paint directly behind the paint spray guns.  The order of application and the application rates of the Type P beads and the wet reflective beads shall be based on the manufacturer’s recommendations to provide wet night retroreflectivity.

3.5  The completed pavement marking system shall meet the initial retroreflectivity requirements of 450 mcd/m2/lux.

3.6  The manufacturer of the wet reflective bead shall have a factory representative on site before the contractor begins striping operations.  The factory representative shall assure the engineer that the wet reflective system has been calibrated for proper application before the contractor begins.  The factory representative shall remain available to periodically assure the engineer the system is being applied according to manufacturers recommendations.

4.0  Method of Measurement.

4.1  Final measurement will not be made except for authorized changes during construction or where appreciable errors are found in the contract quantity.  The revision or correction will be computed and added to or deducted from the contract quantity.

4.2  Where required, measurement of 4 inch, 6 inch, 8 inch or 24 inch pavement marking will be made to nearest linear foot.  Where intermittent lines are specified, deductions will be made for the gaps in pavement marking.

5.0  Basis of Payment.  The accepted quantity of wet reflective pavement markings will be paid at the contract unit price for each of the pay items included in the contract.